# ****Product description****

**Warm edge spacer SWISSPACER Advance**

* Polymer SAN spacer with 35% glass fibre content and thermally improved aluminium foil
* Equivalent thermal conductivity (in accordance with ift guideline WA-17/1): **λ = 0.29 W/mK**
* **Available in a total of 17 RAL-like colours**RAL 9023, 9005, 9016, 5003, 8003, 8014, 1016, 6018, 6026, 7013, 1011, 1034, 6010, 1015, 1001, 7035 or 8012

# ****Performance specification****

**Can be used in multi-pane insulating glass units in accordance with DIN EN 1279**

* Example structures of multi-pane insulating glass units with SWISSPACER Advance:
1. Double-sheet insulating glass (4 – 16 Ar – 4): Ug = 1.1 W/m²K
2. Triple-sheet insulating glass (4 – 12 Ar – 4 – 12 Ar – 4): Ug = 0.7 W/m²K

**Physical values or Psi values (W/mK) for multi-pane insulating glass units with SWISSPACER Advance depending on the window frame materials**

* Representative linear thermal conductivity coefficients (representative Psi values) as defined in ifa guideline WA-08/3 “Thermally improved spacer – Part 1: Determination of the representative Psi value for window frame profiles”

|  |
| --- |
|  |
| Extract from datasheet Psi values windows (August 2014 – No. W24 – Revision index 4-06/2021 – valid until June 30th, 2023) © Arbeitskreis Warme Kante / Bundesverband Flachglas BF |

# Premium product alternative

**Warm edge spacer SWISSPACER Ultimate**

* Polymer SAN spacer with 35% glass fibre content and high-tech gas barrier foil
* Equivalent thermal conductivity (in accordance with ift guideline WA-17/1): **λ = 0.14 W/mK**
* **Available in a total of 17 RAL-like colours**
RAL: 9023, 9005, 9016, 5003, 8003, 8014, 1016, 6018, 6026, 7013, 1011, 1034, 6010, 1015, 1001, 7035 or 8012

# Complementary product

**SWISSPACER AIR for permanent pressure equalisation of insulating glass units**

* The SWISSPACER AIR is a metal sleeve with an integrated special membrane. SWISSPACER AIR was developed as a permanent pressure equaliser in order to be able to transport multi-pane insulating glass units over differences in height and to minimize the distortions of the glass panes due to climatic loads.
* Technical Approval (DIBt) No. Z-70.4-249 of 11 March 2019 for: Pressure-equalised multi-layer insulated glazing with Swisspacer Air pressure equalisation valve

# Manufacturer

SWISSPACER Vetrotech Saint-Gobain International AG
Sonnenwiesenstrasse 15 | 8280 Kreuzlingen, Switzerland
www.swisspacer.com; info@swisspacer.com